## Slide 1: ATLAS/CMS/LCD RD53 collaboration: Pixel readout integrated circuits for extreme rate and radiation
3rd LHCC status report
May 25 2016
RD53 SPs: Jorgen Christiansen, CMS & Maurice Garcia-Sciveres, ATLAS on behalf of RD53

## Slide 2: Reminder RD53
Focussed R&D program to develop pixel chips for ATLAS/CMS phase 2 upgrades and LCD vertex
Extremely challenging requirements for HL-LHC:
  Small pixels: 50x50um2 (25x100um2) and larger pixels
  Large chips: ~2cm x 2cm ( ~1 billion transistors)
  Hit rates: 3 GHz/cm2
  Radiation: 1Grad, 2 1016 neu/cm2 over 10 years (unprecedented)
  Trigger: 1MHz, 10us (~100x buffering and readout)
  Low power - Low mass systems
Baseline technology: 65nm CMOS
Full scale demonstrator pixel chip in 2016.
19 collaborating institutes and many Guests
  Bari, Bergamo-Pavia, Bonn, CERN, CPPM, Fermilab, LBNL, LPNHE Paris, Milano, NIKHEF, New Mexico, Padova, Perugia, Pisa, Prague IP/FNSPE-CTU, RAL, Seville, Torino, UC Santa Cruz. (PSI has withdrawn as very busy with phase 1 pixel upgrade)
  150 on collaboration Email list, 80 on RD53 NDA list (65nm TSMC technology access), 77 on RD53 guests list (ATLAS/CMS people involved in phase 2 pixel but not on chip design) 55 on serial power list (ATLAS/CMS people interested/working on serial powering)

## Slide 3: Internal organization
Before: R&D in working groups:
  Radiation effects and rad hard design
  Analog: Low power/noise/area analog front-ends
  IP blocks: ADC, DAC, PLL, Modified digital library, etc.
  Simulation and architecture: Simulation, Optimization, Verification, ,
  IO: IO interface
  Collaboration meetings across WGs
Now (from 1/1 2016): Focussed on large scale demonstrator
  Project structure for RD53A demonstrator
    Bring everything together to make working large scale chip
  Radiation WG (still a critical issue)
Radiation WG
Analog WG
IP WG
Simulation WG
Top level and chip integration WG
I/O WG

## Slide 4: Radiation effects
Radiation test and qualification of 65nm technology: 1Grad and 2 1016 neu/cm2
  Radiation tests with X-rays, Cobalt source and 3Mev protons
Significant radiation damage above ~100Mrad (only critical for pixels)
  New radiation effects made it difficult to reach clear conclusions
Two major “effects”
  Radiation damage (transconductance) during radiation depends on: Device type, L, W, Bias, Temperature
  Annealing effects depends on: Temperature, Time, Bias, Device type, L, W, Received dose Partial recovery (transconductance) or getting worse (Vt shift)
  (Low dose rate effect)
Realistic to stand 500Mrad with conservative design approach
  Cold detector: -20 - -10 oC, Not getting hotter than room temperature while powered
  Analog: Appropriately designed (large transistors) will only have small radiation degradation
    Confirmed with multiple RD53 prototypes
  Digital: Suffers significant speed degradation as using small transistors
    High density logic in pixel array will have significant (200-400%) speed degradation. Only needs 40MHz operation frequency. High density digital library for pixel array (small modifications of TSMC lib)
    High speed circuits to be designed with large transistors (dedicated digital library)
    Leakage is not a serious problem in 65nm.
    Verification with dedicated digital radiation test chip (DRAD)
  Inner barrel layer to be replaced after 5 years
200/500Mrad simulation models extensively used for circuit simulation and optimization
Full scale pixel chip demonstrator will determine if 1Grad can be accomplished

## Slide 5: A few radiation effects plots
L=1000, W=1000
L=1000n, W=120n
L=60n, W=1000n
PMOS, L=60n, W=600n
L=1000n, W=120n
Radiation Induced Narrow Channel Effect: RINCE (known)
Radiation Induced Short Channel Effect: RISCE (new)
Detrimental annealing effect (new)

## Slide 6: (bad) Annealing
Significant Vt shift can develop with annealing depending on Temperature, Time, Bias, Device type, L, W, Received dose,
  Foundry specific problem ?
Latest's news: Indication that detrimental effect can be “avoided”/delayed by keeping cold
  -20oC for 10years
  Room temp for few months (if unbiased more ?)

## Slide 7: Changing technology ?
High density required in small pixels for hit storage during trigger latency
  130nm technology not sufficient density
Other 65nm technologies will now be tested for radiation damage
  One technology has been seen to have similar radiation damage, but most likely less detrimental annealing (but not any more available)
  Others could be better or worse (unpredictable)
Sub 65nm
  Not yet radiation tested to these high levels
  Significantly increased cost and complexity
We would be “alone” as no other detectors needs to change technology
  Technology access, design kit, support, radiation testing, IPs, shared runs, etc.
RD53 stays with current 65nm technology for large scale demonstrator
  Major design efforts invested in this
  Appears viable for 500Mrad when taking appropriate precautions
  If we are forced to change technology it will take ~1 year to remap design, IPs, FEs, libraries plus extensive radiation testing program will be needed.
Bad combination “avoidance”:
  >200Mrad (inner layer),
    Replace inner layer(s) after 5 years (5% surface)
  Radiation at High/room temperature:
    Pixel will run cold (-10 -20oC)
  Small PMOS: High density digital
    Only needs to run 40MHz
  Analog and Fast Digital circuits:
    Dedicated designs with large transistors
  High/room temperature anneal
    Pixel runs cold
    No bias/power when not cooled
  Needs to confirm that this “avoidance strategy” is sufficient and reliable

## Slide 8: DRAD chip
Dedicated test chip to measure delay degradation and power consumption of digital logic
  RD53, MPA, LPGBT
Test structures with different types of gates: NAND, NOR, buffers, flip-flop, latch
SEU test structure
9 different libraries: 7-18 track
  Small, Mid, Large transistors
  Low Vt, normal Vt, High Vt
  Linear, enclosed
Submitted March. 2016
Return: End May
Radiation test campaign during summer
7T-HVt
9T
9T-HVt
9T-incr
12T
12T-LVt
12T-HVt
12T incr
18T-ELT
Simulated delay degradation (room temp. radiation)
W
Some gates (e.g. 4NOR) more affected than others

## Slide 9: Analog FEs
Low power/noise/area analog pixel Front-Ends
~50% pixel area for analog
Analog front-end specifications defined
  Capacitance, threshold, noise, power, dispersion, etc.
Evaluation of alternative FE architectures
  3 implementations of TOT FEs
    2 slow (40MHz counting) TOT
    1 fast (200MHz counting) TOT
  1 Non linear fast digitizing FE
3 FEs prototyped and extensively tested
  Limited radiation effects

## Slide 10: IPs
Building blocks required to build full pixel chip
  Large diversity of different IP blocks developed
    ADCs, DACs, sensors (temp, current, radiation), Bandgap references, analog buffers, specialized storage cells, PLL, serializers, differential inputs/outputs, shunt-LDO, Power on reset, differential drivers/receivers, etc.
  Specs and data sheets defined
  IPs prototyped and tested.
Large design effort

## Slide 11: Simulation/verification
Simulation and verification framework for pixel chip
  Based on system Verilog and UVM (industry standard for ASIC design and verification)
  Available on repository and being used by several groups
    Reference model
    Basic/generic pixel chip
    Detailed RTL/gate level implementations
    Integration with ROOT to import hits from detector simulations and for monitoring and analysing results.
  Simulation of alternative architectures with Monte Carlo data and/or internally generated hits
    Performance characterization of different architectures
  Verification of small scale prototypes
  Power profiling under different conditions (hits, trigger)
Plans
  Inclusion of SEU simulation/verification
  Detailed verification of demonstrator chip
Buffer occupancy comparison between
simulation and analytical statistical model
25x100um2 pixels

## Slide 12: Pixel array prototypes
FE65-P2: 64 x 64 pixels
  2 x 2 pixel region (evolution from FEI4)
  Low rate readout
  Double Analog / Digital isolation
  4b-ToT with slow (40MHz) FE
  Status: Functional, Under test. Bump bonding to pixel sensor on-going.
CHIPIX65: 64 x 64 pixels
  4 x 4 Pixel Region
  Single Analog / Digital isolation
  5b-ToT with slow and fast FEs
  Includes multiple RD53 IP-blocks
  Status: Submission June 2016
RD53A: 400 x 400(200) pixels
  Status: Under design

## Slide 13: FE65-P2 test results
Before radiation
After 350Mrad

## Slide 14: RD53A
Demonstrator chip:
  Full size chip: ~2cm x 1(2)cm), small pixels (50x50um2), Large pixels, Very high hit and trigger rates, Radiation and SEU tolerance, Effective in-time threshold: 1200e-, Low power, Serial powering, Functional in test beams, etc.
  Specification document agreed with CMS and ATLAS phase 2 pixel communities.
    Pixel sensors compatible with this chip being prepared in both ATLAS and CMS
  Engineering run ~1M$ (we better get this right !)
    Shared run with other project(s) (CMS MPA)
    Demonstrator will be ~1/2 size, but designed as being full size
    Starting to collect required funds (500k$)
Converge all activities in RD53 and WGs on this vital goal/milestone
Schedule:
  Up-scaling small demonstrator: Now
  First version of near final chip: Q3 2016
  Final version: Q4 2016
  (plus some months for extensive verifications)
Core design team: ~10 and increasing
  Weekly design meetings since the beginning of the year.
  Regular 1-2 days getting together
  Defined project structure and responsibilities
  Groups: INFN, Bonn, LBNL, Marseilles, NIKHEF, CERN

## Slide 15: RD53A project structure

## Slide 16: RD53A status
On-going:
  Architecture simulations and optimization using Monte Carlo hit data from experiments.
  Global floor plan: Upscaled small demonstrator
  Shared repositories: IPs, FEs, RTL code, Simulation, full design
  Optimization of design flow & tools for very large complex design
  Integration of FEs (4) with biasing and required adaptions
  Integration of monitoring: ADC, Temp sensor, voltages, currents, etc.
  Integration of serial powering
    Distributed power dissipation, power profiling, decoupling, system simulations
  Integration of IO pad frame
  Digital: RTL coding and technology mapping
    Pixel array: Optimization (power, size, radiation tolerance)
    EOC: Command decoder, chip configuration, readout data formatting, data compression
    Synthesis and timing optimization/verification with radiation effects
    Verification framework
To come:
  SEU optimisation and verification
  Final integration
  Extensive Analog and digital verification
  DRC verification
  Submission

## Slide 17: Summary
Many groups and people working on a focussed R&D effort to implement very high rate pixel chip for extreme radiation
Large number of circuits, building blocks and small pixel arrays have been successfully prototyped and tested in 65nm technology.
Improved understanding of the initially “mysterious” radiation effects seen at extreme radiation levels above 100Mrad
  Many circuits and devices radiation tested
  500Mrad appears as realistic goal
  Test of full pixel chip will determine if 1Grad is feasible when cold
Focussed on submitting full scale demonstrator chip
  Building blocks available and tested
  Extensive experience gained with small pixel array prototypes
  Defined design team with weekly meetings
  Submission: ~End 2016

## Slide 18: Backup slides

## Slide 19: More information
RD53 collaboration meetings: https://indico.cern.ch/category/5036/
ACES: https://indico.cern.ch/event/468486
  RD53 + ATLAS and CMS phase 2 pixel upgrades
Radiation seminar: https://indico.cern.ch/event/442426/
Conferences/workshops
Coming conferences/workshops
  Pixel, Vertex, TWEPP, IWORD, FE workshop

## Slide 20: Top level WG
Architecture and floor-plan for large pixel chip
  Digital sea with analog islands floorplan
    Distribution of power and global signals
    Analog – Digital isolation
  Digital “on-top” design flow
  Pixels – Pixel regions – Pixel cores – End of column
  Implementation of small 64x64 pixel demonstrator in 65nm (submission end of this month)
    Re-optimized “FEI4” for small pixels, higher hit and trigger rates.
Plans
  Refinement of pixel chip (digital) architecture
    Using simulation framework
  Integration of full pixel chip demonstrator
RD53A

## Slide 21: Phase 2 pixel challenges
ATLAS and CMS phase 2 pixel upgrades very challenging
  Very high particle rates: 500MHz/cm2
    Hit rates: 2-3 GHz/cm2 (factor 16 higher than current pixel detectors)
  Smaller pixels: ¼ - ½ (25 – 50 um x 100um)
    Increased resolution
    Improved two track separation (jets)
  Participation in first/second level trigger ?
    40MHz extracted clusters (outer layers) ?
    Region of interest readout for second level trigger ?
  Increased readout rates: 100kHz -> 1MHz
  Low mass -> Low power
  Very similar requirements (and uncertainties) for ATLAS & CMS
Unprecedented hostile radiation: 1Grad, 2 1016 Neu/cm2
  Hybrid pixel detector with separate readout chip and sensor.
  Phase2 pixel will get in 1 year what we now get in 10 years
Pixel sensor(s) not yet determined
  Planar, 3D, Diamond, HV CMOS, , ,
  Possibility of using different sensors in different layers
  Final sensor decision may come relatively late.
Very complex, high rate and radiation hard pixel readout chips required
ATLAS HVCMOS program

## Slide 22: Radiation effects
Charge buildup in gate oxide and interface states affects Vt
Thick Shallow Trench Isolation Oxide (~ 300 nm); radiation-induced charge-buildup may turn on lateral parasitic transistors and affect electric field in the channel)
Doping profile along STI sidewall is critical; doping increases with CMOS scaling, decreases in I/O devices
Increasing sidewall doping makes a device less sensitive to radiation (more difficult to form parasitic leakage paths)
Spacer dielectrics may be radiation-sensitive
Birds beak parasitic device

## Slide 23: Pixel chip generations
Generation | Current FEI3, PSI46 | Phase 1 FEI4, PSI46DIG | Phase 2
Pixel size | 100x150um2 (CMS) 50x400um2 (ATLAS) | 100x150um2 (CMS) 50x250um2 (ATLAS) | 25x100um2 ?
Sensor | 2D, ~300um | 2D+3D (ATLAS) 2D (CMS) | 2D, 3D, Diamond, MAPS ?
Chip size | 7.5x10.5mm2 (ATLAS) 8x10mm2 (CMS) | 20x20mm2 (ATLAS) 8x10mm2 (CMS) | > 20 x 20mm2
Transistors | 1.3M (CMS) 3.5M (ATLAS) | 87M (ATLAS) | ~1G
Hit rate | 100MHz/cm2 | 400MHz/cm2 | 2(3) GHz/cm2
Hit memory per chip | 0.1Mb | 1Mb | ~16Mb
Trigger rate | 100kHz | 100KHz | 200kHz - 1MHz
Trigger latency | 2.5us (ATLAS) 3.2us (CMS) | 2.5us (ATLAS) 3.2us (CMS) | 6 - 20us
Readout rate | 40Mb/s | 320Mb/s | 1-4Gb/s
Radiation | 100Mrad | 200Mrad | 1Grad
Technology | 250nm | 130nm (ATLAS) 250 nm (CMS) | 65nm
Architecture | Digital (ATLAS) Analog (CMS) | Digital (ATLAS) Analog (CMS) | Digital
Buffer location | EOC | Pixel (ATLAS) EOC (CMS) | Pixel
Power | ~1/4 W/cm2 | ~1/4 W/cm2 | ½ - 1 W/cm2

## Slide 24: Working groups
WG | Domain
WG1 | Radiation test/qualification
Coordinate test and qualification of 65nm for 1Grad TID and1016 neu/cm2 Radiation tests and reports. Transistor simulation models after radiation degradation Expertise on radiation effects in 65nm | 
WG2 | Top level
Design Methodology/tools for large complex pixel chip Integration of analog in large digital design Design and verification methodology for very large chips. Design methodology for low power design/synthesis. Clock distribution and optimization. | 
WG3 | Simulation/verification framework
System Verilog simulation and Verification framework Optimization of global architecture/pixel regions/pixel cells | 
WG4 | I/O + (Standard cell)
Development of rad hard IO cells (and standard cells if required) Standardized interfaces: Control, Readout, etc. | 
WG5 | Analog design / analog front-end
Define detailed requirements to analog front-end and digitization Evaluate different analog design approaches for very high radiation environment. Develop analog front-ends | 
WG6 | IP blocks
Definition of required building blocks: RAM, PLL, references , ADC, DAC, power conversion, LDO, , Distribute design work among institutes Implementation, test, verification, documentation | 

## Slide 25: RD53 collaboration
20 Institutes (Seville has joined)
  Bari, Bergamo-Pavia, Bonn, CERN, CPPM, Fermilab, LBNL, LPNHE Paris, Milano, NIKHEF, New Mexico, Padova, Perugia, Pisa, Prague IP/FNSPE-CTU, PSI, RAL, Seville, Torino, UC Santa Cruz.
  140 on collaboration Email list
    ~70 actively contributing
    2015 FTE: ~23
  50 on RD53 guests email list
  Spokes persons: Maurice Garcia-Sciveres, LBNL (ATLAS), Jorgen Christiansen, CERN (CMS)
  IB chair: Lino Demaria, Torino
  WG conveners: Marlon Barbero, Roberto Beccherle, Jorgen Christiansen, Maurice Garcia-Sciveres, Tomasz Hemperek, Valerio Re
  2 year terms coming up to renewal within 3 months
MOU defined and signed (few exceptions)
RD53 collaboration meetings: 2 times per year
RD53 management meetings: Monthly
WG meetings: Monthly – bi-monthly
Activity | FTE 2015
Radiation | 4
Analog | 3
IP | 7
Simulation | 3
Top | 3
IO | 1
Organization | 2
Total | ~23

## Slide 26: Radiation effects (PMOS)
Requires an extended
seminar to explain
all this

## Slide 27: power
400x400 pixels power | Typ | Worst
Analog array | 0.96W | 1.6W
Digital array | 0.77W | 0.99W
EOC | 0.2W | 0.3W
IO | 0.2W | 0.3W
Shunt-LDO | 0.5W (25%) | 1W (30%)
Total | ~3W | ~4W